NTA-functionalized MSP

|  | Product Specifications and Features |
| --- | --- |
| Product Name | MSPs bearing NTA (Ni2+) for 6His-tagged proteins (FBD-MSP-NTA) |
| Manufacturer | Chongqing FBD Biotechnology Co. Ltd., China (http://www.fbdbio.com) |
| Structural properties | paramagnetic noncore Fe3O4, polymer coats bearing zwitterions at pH from 3 to 12, physical diameter of ~0.6m in vacuum while aqueous diameter of ~1.0m, abundant quantity of NTA through long linear arms |
| Performance | good suspension stability, rapid response to external magnetic fields, negligible nonspecific adsorption of proteins; high affinity (Kd at ~pmole/L levels) and large capacity for the binding of 6His tag on proteins |
| Applications | Binding of 6His-tagged proteins for rapid immobilization or isolation |
| Binding capacity | binding > 15 mg 6His-tagged proteins of 60 kD by 1.0 g functionalized MSP |
| Package quantity | FBD-MSP-NTA, 30 g/L; see labels and signs on package |
| Shelf-life | >82 days at 37 0C (closed in dark); > 18 months at 2~8 0C (closed in dark) |
| Storage/shipment | long-duration storage at 2~8 0C; ambient shipment in 7 days |
| Attention | no freezing or acidification; avoiding any treatment causing aggregation |
|  | Binding and Elution of 6His-tagged Proteins |
| Functionalization | To MSP in a large volume of 20 mM MES or HEPES buffer at pH~7.0, was added NiSO4 to final 2.0 mM for 8.0-h adsorption at 25 0C; wash the MSP with the same buffer for three times to remove free Ni2+ |
| Protein Binding | After the removal of wash buffer, proteins in 20 mM Tris-HCl at pH 8.0 were added for 30-min adsorption during mild shaking at 25 0C |
| Protein Elution | Wash of the bound proteins with the same buffer, followed by the addition of 0.10 M imidazole in the same Tris-HCl buffer for mild shaking in 1.0 h to elute proteins. See http://dx.doi.org/10.1016/j.ijbiomac.2014.12.009 |
| Limitations | Applicable to samples of 6His-tagged proteins bearing abundance over 4% |
|  | Safety and Disposal |
| Toxicity | sodium azide in the original suspension; low toxicity of other substances |
| Warning | no swallowing or contact with skin; far away from children; no eating/drinking |
| Emergence | washing skin with lots of water in case of contact; see doctors immediately |
| Environment | no toxicity of the product itself; toxicity of suspension mixture |
| Final Disposal | collection of suspension for treatment; following requirement with product |
| Filed date | 20170616 |