Zwitterion-functionalized MSP

|  | Product Specifications and Features |
| --- | --- |
| Product Name | Zwitterion-functionalized MSP (FBD-MSP-ZEW) |
| Manufacturer | Chongqing FBD Biotechnology Co. Ltd., China (http://www.fbdbio.com) |
| Structural properties | paramagnetic noncore Fe3O4, coats bearing zwitterions at pH from 3 to 12, physical diameter of ~0.6m in vacuum while aqueous diameter of ~1.0m, surface bearing net positive charge at pH 3 but net negative charge at pH 12 |
| Performance | good suspension stability, rapid response to external magnetic fields, negligible nonspecific adsorption of native proteins; binding of negatively charged substances but release of positively charged substances at pH 4.0; release of negatively charged substances but binding of positively charged substrates at pH 9.2; negligible aggregation of suspension after heating at 60 0C for 5.0 min |
| Applications | extraction/isolation of substances bearing negative charges at pH 4.0 (nucleic acids, phosphates, sulfates), or bearing positive charges at pH 9.2 |
| Binding capacity | at pH 4.0, monoanion >20 mole /g; at pH 9.2, monocation >20 mole /g |
| Package quantity | FBD-MSP-ZEW, 30 g/L; see labels and signs on package |
| Shelf-life | >82 days at 37 0C (closed in dark); > 18 months at 2~8 0C (closed in dark) |
| Storage/shipment | long-duration storage at 2~8 0C; ambient shipment in 7 days |
| Attention | no freezing or acidification; avoiding any treatment causing aggregation |
|  | Recommendation for operations |
| Condition | applicable at pH 4.0 ~ 10.0; preferred alkaline pH> 9.0 and acidic pH ~4.0 |
| Usage fields | smaller quantity than Silane MSPs to isolate the same quantity of nucleic acids |
| Optimization | two pH values for adsorption and desorption; heating unnecessary |
|  | Safety and Disposal |
| Toxicity | sodium azide in the original suspension; low toxicity of other substances |
| Warning | no swallowing or contact with skin; far away from children; no eating/drinking |
| Emergence | washing skin with lots of water in case of contact; see doctors immediately |
| Environment | no toxicity of the product itself; toxicity of suspension mixture |
| Final Disposal | collection of suspension for treatment; following requirement with product |
| Filed date | 20170616 |