[image: image1.jpg]Binging capacity of free biotin for
streptavidin magnetic particles

—
wn
S
(=]

—
(]
S
(=]

=)
=
=)

300

Binding capacity (nmol/g)
&
S
(=]




[image: image2.jpg]Binging capacity of biotinylated
alkaline phosphatase for
streptavidin magnetic particles

i i 9
L= 9] (—}

Binding capacity (mg/g)
9]



        Data for Self-testing of FBD-MSP-ZSAV

[image: image3.jpg]Binging capacity of biotinylated
Poly-antibody for streptavidin
magnetic particles

= i b =
= = = =
S S S S

Binding capacity (mg/g)
=]
=
(=]



[image: image4.jpg]ty of biotinylated

alkaline phosphatase (ng)

inging capaci

B

~&- 0208LB-01 11749425 —o- Dynal—-SAV-T1 -e- Dynal-SAV—C1

—o- JSR-SAV —o- Bangs—SAV -o- FBD-ZSAV®)

20 40 60 80 100

Streptavidin magnetic particles (ng)




  �  �


  � �


 � � 





Quantitative comparison of performances of representative MSP-SAV�
�
parameters�
FBD- ZSAV�
Dynal-SAV-C1�
Dynal-SAV-T1�
0208LB-01�
11749425�
JSR-SAV�
Bangs-SAV�
�
Free Biotin (nmol/g)�
1200�
750�
250�
910�
630�
340�
510�
�
Biotin-AP (mg/g)�
17�
10�
3.2�
8.0�
3.3�
0.12�
0.32�
�
Biotin-polyAb (mg/g)�
3.4�
0.79�
0.87�
3.5�
0.86�
0.20�
0.26�
�
quantity for complete isolation of 10 ng Biotin-AP in 30 min (μg)�
~ 5�
＞100�
~ 10�
~ 17�
＞100�
＞100�
＞100�
�
Percentage of 10 ng Biotin-AP isolated after reaction for 5 min�
~90%�
nd�
~ 75%�
~ 83%�
nd�
nd�
nd�
�






FBD-MSP-ZSAV showed rapid binding and high affinities for of biotinylated proteins due to the insertion of long linear arms; the strong hydrophilicity of FBD-MSP-ZCOOH provided hydrophilic surface and no coating with albumin








2
Chongqing Far-sighted-blue-dragon Biotechnology Co. Ltd., the 3rd Keji Road, Xiyong, Shapingba, Chongqing, China; Contact: Gaobo Long, Tel, +0086-23-66562506, E-mail: FBDbiotech@yeah.net


[image: image5.png]Magnetic separation rate

120

100
&
X
= 80
S — FBD-MSP-ZSAV
S 60 — JSR-MSP-SAV
= — Dynal-MSP-SAV-C1
g 40 — Dynal-MSP-SAV-T1
§ — Bangs-MSP-SAV
E 2 — 11749425

~ 0208LB-01
0

0 2 4 6 8 10
Time (min)

12



[image: image6.png]Sedimentation rate

— FBD-MSP-ZSAV

— JSR-MSP-SAV

— Dynal-MSP-SAV-C1
— Dynal-MSP-SAV-T1
— Bangs-MSP-SAV

— 11749425

~ 0208LB-01

0 60 120 180 240
Time (min)



[image: image7.png]L3230
FBD Biotech



