Data for self-testing of FBD-MSP-ZCOOH

Suspension stability

At pH 7.0 in PBS

FBD-MSP-ZCOOH by TEM

Size (0.66  0.15) μm (n = 98)

Aqueous size

Size ~1.0 μm

Magnetic response rate (time for 95% separation)

MSPFBD- ZCOOHJSR-  COOHAB-   COOHBangs-   COOHDynal- COOHTime (min)3.1  0.23.0  0.23.6  0.23.7  0.23.1  0.2

Effects on common enzymes for chemiluminescence immunoassay

Saturated conjugation of polyclonal antibodies to isolate antigen ECAP

Surface of zwitterions for strong hydrophilicity, Fe3O4 nanocores, swelling in water, carboxyl group ~20 mole/g through long linear arms, streptavidin reserved nearly 75% activity after conjugation