Carboxyl functionalized MSP

|  | Product Specifications and Features |
| --- | --- |
| Product Name | MSP bearing positive charges after carboxyl activation (FBD-MSP-ZCOOH) |
| Manufacturer | Chongqing FBD Biotechnology Co. Ltd., China (http://www.fbdbio.com) |
| Structural properties | paramagnetic noncore Fe3O4, polymer coats bearing zwitterions at pH from 3 to 12, physical diameter of ~0.6m in vacuum while aqueous diameter of ~1.0m, long linear arm between MSP and aliphatic carboxyl group, net positive charges at neutral pH after the activation of carboxyl group |
| Performance | good suspension stability, rapid response to external magnetic fields, negligible nonspecific adsorption of proteins; high conjugation capacity and efficacy of proteins bearing pI lower than 6.0 even at low concentrations |
| Applications | conjugation of proteins bearing pI lower than 6.0 |
| Binding capacity | conjugation of ~15 mg proteins bearing 60 kD molecular weight to 1.0 g MSP for nearly 75% of their original activities before conjugation |
| Package quantity | FBD-MSP-ZCOOH, 30 g/L; see labels and signs on package |
| Shelf-life | >82 days at 37 0C (closed in dark); > 18 months at 2~8 0C (closed in dark) |
| Storage/shipment | long-duration storage at 2~8 0C; ambient shipment in 7 days |
| Attention | no freezing or acidification; avoiding any treatment causing aggregation |
|  | Activation and Conjugation of Proteins |
| Buffer solution | 20 mM 2-(N-morphilino)-ethanesulfonic acid (MES), at pH 6.0 or optimized, for carboxyl activation, MSP wash, and protein conjugation |
| Two activators | EDC and NHS at final 50 g/L in the buffer, separately; storage at 2~8 0C |
| Activation | 0.10 g MSP-ZCOOH plus each activator of 10 ml; 25 0C for ~30 min |
| Washing process | with the pre-cooled buffer, wash twice in 15 min, shaking |
| Dispersion | dispersed vigorously to <10 g/L in the buffer, for use in 30 min |
| Conjugation | 0.1 g MSP + equal volume of a protein (< 0.6 g/L), 25 0C for 30~60 min |
| Termination | 0.10 M glycine in the same buffer; kept at 25 0C for 30~60 min, shaking |
|  | Safety and Disposal |
| Toxicity | sodium azide in the original suspension; low toxicity of other substances |
| Warning | no swallowing or contact with skin; far away from children; no eating/drinking |
| Emergence | washing skin with lots of water in case of contact; see doctors immediately |
| Environment | no toxicity of the product itself; toxicity of suspension mixture |
| Final Disposal | collection of suspension for treatment; following requirement with product |
| Filed date | 20170616 |